## Slide 1: Matrix X

## Slide 2: MATRIX X
Matrix X Dc 220, 300
Matrix X AcDc 220, 300, 400, 500
New XV user-interface (= X.Vision)
Also available -- with conventional operation-panel
u/d torches (parameters + jobs)
Very stable/reliable ignition
DC – 1A min.current
AC – 3A min.current
Perfect-Point … best-possible Spot-Position
Repeated-Ignition Function
Ignition - always on positive wave (AC)

## Slide 3: RCT … Running Cold Tack
COLD TACK => RCT Running Cold Tack - on DC
For thin sheets
Minimal thermal input – compared to (puls) TIG
Default-Setting
  Amperage => max.
  Tack-Time
  Pause-Time => 1 sec (to avoid malfunction of automatic helmets)
  Quan. of Impulses => 1 (max. 10)

## Slide 4: PULS-modes
SYN (Easy-Puls)
  Synergic Puls - based on set peak current.
  Simple
  DC
SLOW
  Peak / base current + time - individually adjustable
  Optimal filler-deposition => good look
  Useful – in combination with BALANCE / Frequency
  AC / DC
FAST
  0,5 - 500 Hz for more concentrated arc cone!
  Smaller arc-diameter
  Less deformation
  DC
ULTRA-FAST
  Up to 2000 Hz
  DC

## Slide 5: AC wave-forms
DYNAMIC
  Rectangular wave
  Most common
  High arc stability
  Small-medium thickness
COLD
  Triangular Wave
  Low heat transfer -- with reduced deformation
  Small thickness
SOFT
  Sinusoidal wave
  Silent an soft arc
  Butt welding joints
SPEED
  Mixed Wave
  Good penetration at high welding speed
  Big thickness
  Longer electrode life
Overview
  Rectangular DYNAMIC TIG … for all applications
  Triangular COLD TIG … for small thickness
  Sinusoidal SOFT TIG … for low noise
  Mix wave-form SPEED TIG … for high speed / long electrode-life

## Slide 6: Balance / Frequency
Balance
  Positive and negative wave – separatly adjustable
  Pos / Neg – power
  Pos / Neg – time
  Proportion of Pos / Neg wave
AC Frequency
  High frequence => very thin sheets, high welding-speeds (automatic use)

## Slide 7: Tungston-Electr. Diameter
Elektrode-diameter adjustable
  Iginition-Courrent adjusted
  Shaping of ball (‚calotte‘)
MMA – also in AC possible
  To avoid blowing-effect
  Hotstart and Arcforce adjustable

## Slide 8: Cycle-function
Switching between 2 set Amp-levels – by torch-trigger

## Slide 9: MATRIX - accessories

## Slide 10: Matrix X
Very small and compact
300A version …. 17kg

## Slide 11: Matrix X
Modern Cooling-concept
High duty-cycle (60% - 400A/500A version)
No metalic dust on electronic components
Less maintenance

## Slide 12: Matrix X – for robotic/automatc use
….

## Slide 13: Matrix X - target-group
.